## Slide 1: Experiment-fit time-domain modeling of high-optical-gain dyes for active plasmonic nanostructures Nikita Arnold1, Ludmila Prokopeva2,3, Thomas A. Klar1, Alexander V. Kildishev2
1 Institute of Applied Physics, J. Kepler University, Linz, Austria
2 Birck Nanotechnology Center, School of ECE, Purdue University, USA
3 Institute for Computational Technologies, SB RAS,
Novosibirsk, Russia
Notes: 1

## Slide 2
2
Why model dyes in nano-plasmonics?
Limiting factor: losses. Proposal: fight losses with gain1
Y
X
Silver
Al2O3
Gain material
H
1Klar, Kildishev, Drachev, Shalaev, IEEE J. of Sel. Top. in Quant. Electr. 12, 1106 (2006)
2Xiao, Drachev,Kildishev, Ni, Chettiar, Yuan, Shalaev, Nature 466, 735 (2010)
3Trieschmann , Xiao , Prokopeva, Drachev, Kildishev, Opt. Express 19(19) 18253 (2011)
4Prokopeva, Bornemann, Kildishev, IEEE Trans. Magn. 47(5), 1150 (2011)
Experimental proof: high losses require high gain:
lossless fishnet with Rh8002
Aims of detailed modeling:
  Experiments, new physics, devices
Challenges:
  Dispersion, population dynamics
  Multiphysics: saturation, NL effects, e-phonons-T, phase changes, chemistry, etc. - all evolve in time
Numerical requirements:
  Unified description for dispersion and gain
  Algorithms: minimize flops, scalability, parallelization, stability, accuracy
  Applicable to FDTD (structured mesh), FVTD and FETD (shape-conformal unstructured meshes)
Time domain
Numerical issues are scarcely addressed in literature3,4
Notes: 2
Limiting factor for almost any figure of merit in plasmonics and metamaterials – field enhancement, spatial localization, imaging

## Slide 3
Dispersion: from a Pade approximant to physical terms
  () - arbitrary Pade
  Partial fraction decomposition
Conductivity
Debye
Lorentz, Sellmeier, CP
Drude
Frequency-Domain
Simple terms in p(t)=()*E(t-) convolution are calculated recursively
Time-Domain
  aj– amplitude, j – phase, δj –oscillation, γj – damping
Notes: Pade – rational ratio
a, b coefficients real, as they stem from physics
(…  ) irrelevant in some Fourier transforms as they are usually at unphysical , e.g., at =0, for conductivity term

## Slide 4
≈
n-kEk with k=ck-1
Dispersion: Universal time-domain implementation
Recursive Convolution (RC)
=
Different RC approx. lead to different FD schemes
Similar FD Equations for both ADE and RC. 2-3 stencil, 2nd order
Invert () terms 
Auxiliary Differential Equations (ADE):
Drude, Debye, Lorentz, Sellmeier, Critical Point (CP)
1
Finite-Difference (FD) approximation
■ all Models in one framework
■ less parameters ■ less flops (>30%)
Dispersion section is published in IEEE Trans. Magn. (2011) 47-5
Notes: Explain physics – Drude electron, Debye damping, Lorentz oscillator, etc. Hint how they appear from () expressions
c – usually e - recursive accumulator. Different RC schemes depend on the approximations used in integration (of these simple functions) and differ in first 2  terms
PCRC – piecewise constant RC
PCRC2 – piecewise constant RC of the second order
PLRC – piecewise linear RC
TRC – trapezoidal RC
RRC – rectangular RC
4

## Slide 5
Full p-N: Siegman, Lasers, (1986);
DM: Rautian, Shalagin, Kinetic Problems of Nonlinear Spectroscopy (1991) AND Boyd, Nonlinear Optics (2008);
Polarizations:
Lorentz oscillators with N(t)
Polarizations are coupled to Maxwell’s equations
Full p-N
system
From dispersion to gain
Lorentzian example: 4 level scheme for Rh800
Populations dynamics
Fast driving terms
(energy exchange)
3
2
1
0
r21~6.3ns
10~0.35ps
32~0.3ps
pumping, K30~29ns
695 nm, 30~9fs
lasing, K21~6.3ns
723 nm, 21~3.75fs
nr21~262ps
Notes: ADE-FDTD: Zhukovsky and Chigrin, Phys. Stat. Sol. 244, 3515 (2007)
(Yee’s scheme)
5

## Slide 6
pulse=2ps
pump=695nm
probe=720nm
Parameters retrieval for gain medium1
Simulations: 4-level p-N scheme
+ 1D Maxwell
Different pulse durations (time dynamics)
Different wavelengths (spectral behavior)
RMS fitting for probe=720nm  model parameters
Key parameter: r,21+ measured 
1Trieschmann , Xiao , Prokopeva, Drachev, Kildishev, Opt. Express 19(19) 18253 (2011)
2D. P. Benfey et al., “Diode-pumped dye laser analysis and design”, Applied Optics 31, 7034 (1992)
Experiment: dependence of probe transmission on pump intensity
Rh800 in epoxy solid film. No literature values (only e.g., methanol host2)
Pump-probe:
Different probe (703…726nm)
Different pulse (103fs, 2ps)
Rh800/ethanol reference for quantum yield 
Result: All parameters are close to methanol values, apart from 
Chemical environment affects NR lifetimes
nr,21
0.26ns
nr,212
0.77ns
Notes: Two curves are with and without  term in population equations
Host is important as it influences kinetic dye parameters
Water creates white light that is used only in probe before the filter (it has low intensity)
Intensity scale was effectively fitted in calculations as it is difficult to directly measure it, especially inside the gain medium
One can argue about the absolute amplification, but the signal was definitely enhanced with respect to “no pump” case
Probably dye was to thin for strong effect
There is competing absorption tail on the emission lime, also FP and other 1D effects
6

## Slide 7
Levels of description:
QM: ( or ), Full p-N, SVEA, Rate equations, ()
Full p-N
Energy exchange
SVEs
Complex SVEs
Rate
Lorentzian absorption/emission
Rate equations: fail for short pulses, coherent effects
SVEA
SVEA: average over Tlight, always works,
is ~101-2 times faster
Notes: 7
Analytic signal from the field of signal processing
For CARS all frequencies important

## Slide 8
Examples of Rh800 dynamics and () recovery
=10fs, 30abs=695nm
E=108V/m - “weak” field
-0.02
-0.01
0
0.01
0.02
Real
Polarizabilities
gain
3
0
analytical
650
660
670
680
690
700
710
720
730
740
750
0
0.01
0.02
0.03
0.04
wavelength, nm
Imag
”30 saturates
-0.02
-0.01
0
0.01
0.02
Real
Polarizabilities
gain
3
0
analytical
650
660
670
680
690
700
710
720
730
740
750
0
0.01
0.02
0.03
0.04
wavelength, nm
Imag
Lorentzian
”30 absorption
30 saturation
E=109V/m
post-pulse 21 inversion
Notes: 8

## Slide 9
Coherent effects for 30 transition in Rh800
3
2
1
0
r21~6.3ns
10~0.35ps
32~0.3ps
pumping, K30~29ns
695 nm, 30~9fs
lasing, K21~6.3ns
723 nm, 21~3.75fs
nr20~262ps
=50fs, 30abs=695nm
E=109V/m (I=2.21011W/cm2)
32 relaxation
21 inversion
Coherent 30
inversion
Rabi terms
Notes: 9
3-2-1 relaxation after the pulse
Appreciable susceptibility – see previous slides
P in SI units, =P/E00, 0=8,810-12

## Slide 10
10
All 4 levels are needed to describe high-I absorption
Rh800, =1ps, 30abs=695nm
E=109V/m (I=2.21011W/cm2)
0
1
2
3
4
5
6
7
0
0.2
0.4
0.6
0.8
1
N
3
N
2
N
1
N
0
0
1
2
3
4
5
6
7
-3
-2
-1
0
1
2
3
x 10
-5
t, ps
P
2
1
P
3
0
sum
when 30 is saturated
p21(30)>p30
3
2
1
0
r21~6.3ns
10~0.35ps
32~0.3ps
pumping, K30~29ns
695 nm, 30~9fs
lasing, K21~6.3ns
723 nm, 21~3.75fs
nr20~262ps
t, ps
3.465
3.47
3.475
3.48
3.485
3.49
3.495
3.5
0.23
0.24
0.25
0.26
0.27
N
3
N
2
N
1
N
0
3.465
3.47
3.475
3.48
3.485
3.49
3.495
3.5
-4
-3
-2
-1
0
1
2
3
4
x 10
-6
t, ps
P
2
1
P
3
0
sum
10-6
Transition 30:
at resonance, saturated
Transition 21:
off-resonance, inverted,
p21(=30) has phase shift
Total p=p30+p21<p30,21
Notes: 10

## Slide 11
31
2
11
0
pumping
K3(1)0, K3(2)0
lasing
K21(1),K21(2)
12
32
10
nr20
32
11
Asymmetric Lorentzians (CP models), virtual levels for MP absorption1
Realistic models should include:
N(t)-saturation, coherent effects (Rabi)
Multilevels, vibronic sub-lines with spectral “mirroring”
Which  to keep? Physics: non-radiative relaxations to vibronic bottoms, radiative “vertical”
Do we need such details?
To pinpoint plasmonic resonances
To quantify modifications of dye parameters by metals (Purcell effect, etc.)
1SPIE Proc. (2011) 8172-10
Complex dyes: beyond single Lorentzian
Notes: 11
1-Bilinear numerical scheme for improved stability
The corresponding tools will be added to nanohub.org

## Slide 12
466
0.61
513
1
555
0.17
486
0.59
=438
1
HWHM
4.7, 12fs
HWHM
11, 5.3, 8fs
12
31
2
11
0
32~1ps
r3(1)0, K3(1)0~55ns, 466nm
pumping
K21(1)~84ns, 486nm
lasing
12
32
10~1ps
nr20~2.9ns
r21(2)~23ns
r21(1)~84ns
r3(2)0, K3(2)0~13ns, 438nm
K21(2)~23ns, 513nm
Experiment (Dr. B. Ding): τfluor = 2.53ns,
σabs 10-16cm2, =0.14, n“=0.01 (OD @2), =2.3103 cm-1, Ntot=2.3 1019 cm-3
6-level scheme example:
“Thermo Scientific Green Fluorescent Dye” in PS film
Notes: 12

## Slide 13
Fine spectral structure
All polarizations (lines overlap)  recover separate terms
Frequency scan for longer pulses
(),()-recovery for 6 level scheme. 3fs pump-probe pulses
0
0.5
1
1.5
2
2.5
0
0.05
0.1
0.15
0.2
N3
2
N3
1
N2
N1
2
N1
1
N0
0
0.5
1
1.5
2
2.5
-2
-1
0
1
2
x 10
-4
t, ps
sum
P3
2
0
P3
1
0
P21
2
P21
1
2
2.005
2.01
2.015
2.02
2.025
2.03
2.035
2.04
2.045
-5
0
5
x 10
-5
t, ps
320=438nm
2109 V/m
212=513nm
109 V/m
del=2ps
-0.01
-0.005
0
0.005
0.01
0.015
Real
Polarizabilities
400
420
440
460
480
500
520
540
560
580
600
0
0.005
0.01
0.015
0.02
wavelength, nm
Imag
sum
gain3
2
0
gain3
1
0
analytical
”
<analyt -saturation
’
pump
-0.002
-0.001
0
0.001
0.002
Real
Polarizabilities
400
420
440
460
480
500
520
540
560
580
600
-0.004
-0.003
-0.002
-0.001
0
wavelength, nm
Imag
sum
gain21
2
gain21
1
”<0
-inversion
’
probe
Notes: 13
When pump saturates, probe signal is clearer
There exist numerical problems, short pulses, stability, etc. – they are all resolved

## Slide 14
6 level scheme, 4m slab. Full p-N+1D Maxwell, pulse=50 fs
Probe R, T, A as a function of pump-probe delay
Pump: E=3109V/m, pump=438nm (main line), Probe: E=107V/m
delay dependence reflects relaxation times 3(1,2)2=1ps
Both emission sub-lines are inverted (A<0), but:
T(513) is amplified (T>1), while T(486) is only enhanced (T>Tno pump)
For ns delay the depopulation of upper emission level 2 settles in
probe=513nm
main line
probe=486nm
weaker line
Notes: 14
At longer, ns range times one can see depopulation of the upper emission level
2=(r21(1)+r21(2)+nr20)-1

## Slide 15
6 level scheme, 4m slab. Full p-N+1D Maxwell, pulse=50 fs
Probe R, T, A as a function of pump intensity
Pump: 109<E<1010V/m (pump=438nm), delay=5ps, Probe: E=107V/m
Fabry-Perot and other 1D effects are important in R,T,A()
T(513) is inverted (A<0) and amplified (T>1) at lower Epump than T(486): 486nm is weaker and has stronger absorption overlap
Epump dependence reflects saturation fluence
for 320 absorption:
probe=513nm
main line
probe=486nm
weaker line
Notes: 15
Saturation intensity with relax (probably 32 in this case – have a look in SVEA) instead of pulse for longer pulses

## Slide 16
Unified numerical modeling of dispersive media
Unified modeling of gain media
- parameter retrieval for gain media
- asymmetric Lorentzian line shapes
- arbitrary multilevel (ML) schemes
IEEE Trans. Magn. (2011) 47-5
Description levels: Full p-N system, SVEA, Rate eqns., coherent and ML effects
6-level system example: ()-recovery, pump-probe transmission dependence on delay, Epump
Gain I
Dispersion
Gain II
Summary
SPIE Proc. (2011) 8172-10
Opt. Express (2011) 19(19):18253-9
Not published
Notes: 16

## Slide 17
Thank you for your attention
Funding: ERC grant Active NP 257158
ARO MURI award 50342-PH-MUR
ONR MURI grant N00014-10-1-0942
AFRL Materials and Manufacturing Directorate Applied Metamaterials Program
Notes: ERC European Reseach Council
ARO Army Reseach Office
ONR Office of Naval Research
MURI Multidisciplinary University Research Initiative
AFRL Air Force Research Laboratory
17