## Slide 1
ABLATIVE THRESHOLDS IN LASER CLEANING
OF SUBSTRATES FROM PARTICULATES
N. Arnold, G. Schrems, D. Bäuerle
Angewandte Physik, Johannes - Kepler - Universität
A-4040, Linz, Austria

## Slide 2
Summary:
Thermal expansion models of dry laser cleaning (DLC)
Holes under the particles
Field enhancement overview
Local ablation thresholds
Principal limitations for damage-free DLC
Influence of humidity

## Slide 3
Principle of dry laser cleaning1
1Zapka, Tam, Appl. Phys. Lett., 91
short
laser
pulse
Fast thermal expansion
Before
After
Notes: Real particles are non-spherical, but spherical particles are often used for controllable and reproducible experiments, that allow quantification.

## Slide 4
1D+3D expansion
  heavy particles: elastic energy Eelastic>Eadhesion
  small particles: force of inertia Fcleaning>Fadhesion
Removal conditions:

## Slide 5
Thermal expansion: theory and experiment
SiO2/Si, n=1.5
=248 nm
=27 ns
Schrems, Mühlberger, et. al, Proc. SPIE, (2002)
* Laser Cleaning, Luk'yanchuk ed., (2002)
1D too weak
3D OK*
wrong slope:
local ablation

## Slide 6
Damage – common in DLC
Different materials, pulse lengths, wavelength
SiO2/Si, 1500 nm,
 = 500 mJ/cm²  cl
=1064 nm, 6 ns
PS/Si, 800 nm,  ~25 mJ/cm²
=800 nm, 30 ps
Mosbacher, Münzer et. al., Appl. Phys. A, 2001
Schrems, PhD thesis, Linz, 2002

## Slide 7
PS/Si, 800nm, f ~25 mJ/cm²
=800 nm
100 fs
8 ns
Al2O3/Si, 400 nm
=800 nm
800 nm
fs holes better localized
Irregularly
shaped particles:
150 fs
Leiderer, Boneberg, et al, Proc. SPIE, 2000
Münzer, Mosbacher, et. al, Proc. SPIE, 2002

## Slide 8
Optical problem:
Small particles – near field dipole
Large transparent particles –geometrical + diffraction optics, caustics, Mie calculations
Arrays of large particles not in contact with the substrate can be used for different types of parallel surface processing (ablation, deposition, etching, modification)*
*Denk, Piglmayer, Bäuerle, Appl. Phys. A, Appl. Phys. Lett, 2002, 2003

## Slide 9
Small particle – near field dipole
r=0.2; n=1.5
spot wd r
additional 3D intensity Id/I0  r2
Holds also for non-spherical particles
3D
laser
Ex

## Slide 10
Large particle -- geometrical optics
spot wg r
intensity Ig/I0 - independent on r
r>>; n=1.5
Ig near the surface
Caustic cone
Transparent particle

## Slide 11
Focusing of sagittal rays  central caustic line (here in Mie calculations*)
*Program by Wang, Luk’yanchuk, DSI Singapore
Spherical particle

## Slide 12
Intensity under a SiO2 particle r = z =3.1 µm n=1.4, =248 nm. Mie parameter kr=78.54.
Central caustic line*
Ic~kr, wc~/5, P/P~(kr)-1
Caustic cone*
Ico~(kr)1/3, wco~2/3r1/3, P/P~(kr)-1/3
stable
Geometrical region
Ig~C(n), wg~r, P/P~1
What determines Tmax depends on pulse duration 
*based on: Kravtsov, Orlov
Caustics, catastrophes and wave fields, 1998
Shadow

## Slide 13
Local 3D effects*
Thermal expansion
cleaning threshold
Ablative
cleaning threshold
Intensity
Dynamics of particle
3D thermal expansion
Local ablation ~1.5Tb,
momentum transfer
Temperature
*Luk’yanchuk, Arnold, et al, Appl. Phys. A, 2003
Notes: Particle substrate heat exchange is difficult, especially if we take into account that contact radius changes, etc.

## Slide 14
Feasibility of ablative cleaning of particles
Actual pressures higher (lateral expansion, losses)
Such pressures are attainable within narrow interval of Tmax~1.5 Tb
Force criterion: pS>Fadhesion
Energy criterion pV>Eadhesion
Conditions for the pressure p
Notes: Liquid if present

## Slide 15
Focusing: intensity and temperature
ns pulses, r>3:
Imax due to caustic
Tmax due to geom.
(larger power)

## Slide 16
Comparison with the experiment SiO2/Si, ablative mechanism
- KrF, =248 nm, Vacuum*
=27 ns, A=0.39, l=6 nm, lT=0.8 µm, np=1.5
3D calculations
Thermal expansion - wrong
Ablation-correct slope
Discrepancies:
Substrate influence
Parameters (T-dep., particles stoichiometry)
*Schrems, Mühlberger, et. al, 2002
Rescaled to Mie

## Slide 17
Nd-YAG2, =532 nm, Vacuum*
=8 ns, A=0.63, l=0.1 µm, lT=0.45 µm
, lT , l, r/ , A change 
3D part different
Ablation - correct slope
*Bertsch, Mosbacher, et. al, 2002

## Slide 18
Nd-YAG, =1064 nm, Vacuum*
=8 ns, A=0.7, l=17 µm, lT=0.45 µm
Strong (T)
Large uncertainties, but
Ablation-correct slope
*Schrems, Bäuerle et al. 2003

## Slide 19
How to avoid local damage

## Slide 20
Larger substrate l is better for damage-free cleaning
Optimal absorption length and pulse duration
Why?
expansion l Tdz 
Larger with the same surface temperature Ts
T(z)
Ts<Tm

## Slide 21
Small particles are interesting
They weakly disturb the local field (small dipole moment)1D
Sizes that can be removed
 - work of adhesion
 - thermal expansion coefficient
Maximum expansion till melting l<1Tm(l+lT)
They are removed in the force regime ml/ 2>Fadhesion

## Slide 22
Si:
l(193,248,308)5-10 nm
l(1.06)  200 µm50 nm
l(2.94)  500 cm30 µm (depending on doping and T)
l(10.6)  1000 µm100 nm
in µm, ns:
 =100 ps
l=1 µm
Q-switch
l=100 µm
Excimer
l=10 nm
Er or other IR with  ~100 ps

## Slide 23
d =3280 nm,  = 280 mJ/cm²  cl
d =1500 nm,  = 500 mJ/cm²  cl
d=990 nm,  = 675 mJ/cm²  cl
d = 990 nm,  = 675 mJ/cm²  cl
Nd-YAG 1064 SiO2/Si Experimental results
Schrems, Ph.D thesis, Linz, 2003
Notes: Unfortunately, upon detailed examination one finds either holes in the substrate or debris from the exploded particle.

## Slide 24
cl = hole formation for 2r > 1500 nm
990 nm SiO2 particles melt around cl
Nd-YAG 1064 nm: Results and Conclusions
Particles absorb at 1064 nm (probably SiOx  color centers).
Nd-YAG is NOT suitable for cleaning of colloid SiO2 particles other particles/wavelength should be considered

## Slide 25
Cleaning in vapor atmosphere
Steam laser cleaning:
Explosive evaporation of thin liquid layer
Removes small particles, but:
poor reproducibility
Spin-on, film inhomogeneities
film unstable - evaporates, difficult to control,
synchronization with the laser pulse
Contaminates all surface
Use capillary condensation
occurs below 100% relative humidity (RH)
stable liquid meniscus
liquid is only where it is needed
Kelvin
Radius RK

## Slide 26
Capillary condensation
Sl
Vl
RK
r
Liquid-particle surface
Liquid volume (wetting)
Capillary adhesion force
Independent on RH
Meniscus is stable. Kelvin radius:
 - surface tension, µ - molar weight
Notes: Note linear dependence on r

## Slide 27
Experimental Setup
pump
cooling
trap
distilled water
entrance window
target
reaction
chamber
valve
valve
KrF laser
pulse
93%  RH  97%
25°C  T  28,5°C
31mbar  p  35mbar
hygrometer
thermometer
barometer

## Slide 28
KrF, =248 nm, RH vs Vacuum*
=27 ns, np=1.5, RH0.95
*Schrems, Bäuerle et al, 2003
With RH:
Larger particles cl~const
Smaller particles cl
Tclean gradually decreases
Why?
holes with large particles remain

## Slide 29
Water meniscus drawn in scale
n=1.4, RH=0.95
Kelvin radius RK=10 nm
Vwater>Vablated material for smaller r
turnover at:
Size r= 2.5 µm
Size r= 0.15 µm
Notes: One can think of a tricky mechanism: Water a) increases adhesion by adds capillary force b) decreases adhesion as such by decreasing work of adhesion by polar molecules. When everything is cold, adhesion is increased, via capillary. But as we heat near critical temperature, capillary contribution disappears due to vanishing surface tension and we are left with pure decrease of adhesion.

## Slide 30
Conclusions for cleaning with RH0.95
Large particles (2r=5000, 3280 nm)
Ablation of substrate is dominant 
cl const(RH)
Small particles (300 nm – 800 nm)
Removed more efficiently in RH - large contribution of explosively vaporized water

## Slide 31
Conclusions
Overview of field enhancement by transparent spherical particles is presented
Model based on local ablation describes cleaning thresholds better than thermal expansion
Principal limitations for damage-free DLC are considered. For Si, substrate absorption weaker than that of excimer lasers is advantageous. Move to IR and sub-ns pulses is suggested
High RH improves cleaning of small particles, hinders that of average particles and has no effect on large ones. This is attributed to gradual contribution of capillary condensed water to ablative cleaning.

## Slide 32
Singapore
Prof. B. Luk’yanchuk, Prof. M. Hong, Dr. Z. B. Wang
Konstanz
Prof. P. Leiderer, DI. M. Mosbacher, Dr. H.-J. Münzer, DI. M. Olapinski
Sydney
Prof. D. Kane, Dr. S. Pleasants
Linz
Prof. D. Bäuerle, Dr. M.P. Delamare, DI. G. Schrems, Dr. K. Piglmayer
Funding:
EU TMR Laser Cleaning, #ERBFMRXCT98 0188, coordinator Prof. R. Oltra, Dijon
Austrian Science Fund (FWF), P14700-TPH
Acknowledgments