## Slide 1
LASER CLEANING OF SMALL PARTICLES
N. Arnold
Angewandte Physik, Johannes - Kepler - Universität
A-4040, Linz, Austria

## Slide 2
Summary:
Principle of dry laser cleaning
Adhesion potential and cleaning force
Thermal expansion
3 cleaning regimes
Resonance effects
Focusing, 3D heating and expansion
Local ablation
Steam laser cleaning
Influence of humidity
Cleaning with laser-induced SAW
Influence of storage time

## Slide 3
Principle of dry laser cleaning1
1W. Zapka, A. Tam, Appl. Phys. Lett., 91
short
laser
pulse
Fast thermal expansion
Before
After
Notes: Real particles are non-spherical, but spherical particles are often used for controllable and reproducible experiments, that allow quantification.

## Slide 4
BACKGROUND:
Removal of inorganic and organic particulates from solid surfaces (microelectronics, micromechanics, sensor/ actuator technology, optics... )
MODEL SYSTEMS:
Mainly spherical particulates (metals, semiconductors, insulators, polymers) on solid surfaces

## Slide 5
Killer defects below 100 nm
Traditional cleaning methods are complex
Clean smaller particles with alternative methods
Dynamic effects in the detachment of particles
Unified approach and compact formulas
Motivation and goals

## Slide 6
- In all cases strong dependence on fluence and particle size
- Threshold for cleaning, Cl
- Cl increases with decreasing particle size r
- Strong influence of atmosphere

## Slide 7
RH 
27 %
DEPENDENCE ON FLUENCE AND PARTICLE SIZE
Substrate absorption
Particle absorption
RH 
27 %
T.Fourrier, G.Schrems, T.Mühlberger, J.Heitz, N.Arnold, D.Bäuerle, M.Mosbacher, J.Boneberg, P.Leiderer: Appl.Phys.A 72, 1 (2001)

## Slide 8
Particle removal requires Kcl  Kad
Kc = 2r 
(cos 1 + cos 2 )
U = contact pot.
difference
Point cont. F   a r

## Slide 9
-S
VYu2
h
Adhesion potential
Force measurements - static
Laser cleaning – dynamic1-6  potential is important
Potential7
- <Young modulus>
 - work of adhesion
This potential is a smooth function
1Y. F. Lu et al., Appl. Phys. A, 99
2G. Vereecke et al., J. Appl. Phys., 99
3V. Dobler et al., Appl. Phys. A, 99
4D. Bäuerle, Laser Processing and Chemistry, 00
5V. Veiko et al., SPIE, 00
6B. Luk’yanchuk et al., Proc. SPIE, 01
7N. Arnold et al., Proc. SPIE, 01
Notes: There exist more complicated descriptions of adhesion, for example DMT and JKR. The main parameter there is Muller parameter. It is y/h0, where y is the distance from the surface where VdW pressure equates tensile stress: Yy/a~/. Here a is contact radius and  range of action of VdW forces (about interatomic distance). All estimations neglect y in the first order. DMT is Muller<<1, hard spheres (F=2r), and JKR is Muller>>1, soft spheres (F=3/2r) with this hysteresis
Note that in some notations if not the work of adhesion but energy of a single surface is used for , the result is doubled.
Elasticity from Hertz contact problem. It is derived in general for 2 spheres with reduced radius. Both substrate and sphere are deformed and softer material is deformed stronger. Elastic energy is also stored in softer material with smaller Y. It all can pretty well be understood thinking in terms of 2 springs with different spring constants.
In reality area is different, but interaction energy extends, further, there exists a hysteresis, like in AFM tip-substrate interaction.
The key is that equations of 3D elasticity include Laplacian. It decays like 1/r. Therefore the volume is about a3 and strain h/a. This is enough to derive the qualitative behavior. Show it

## Slide 10
Characteristics of adhesion potential
0
U0
F0
h0
Notes: Orders of magnitude (for r~1 µm)
F~0.04 dyn=410-7 N=400 nN
U0~ 10-9 erg= 10-2 J
h0~ 310-8 cm= 0.3 nm
a~ 310-6 cm= 30 nm
m~ 10-11 g
For macroscopic spheres, say 1 cm, all laws are different, as gravity starts to play an important role, when mg>F0. This is with r>1 mm

## Slide 11
Equation of motion for h
Deformation h depends on the expansion of
substrate l and particle r
Laboratory displacement of the particle center z
Adhesion cleaning
+elasticity
Particle and
substrate expansion
enter together
z
l
r
h
Notes: Some other terms like dl/dt, dr/dt, are usually of smaller order, unless damping is too strong.
Expansion of the substrate can be readily interpreted as force of inertia in non-inertial system moving with the surface.

## Slide 12
Viscosity
Big particles, liquids, Stokes
 dynamic viscosity
Knudsen viscosity
r smaller than mean free path
ma mass of gas molecules
N number density
Absorption of sound
Sound generated by thermal
expansion may be damped.
d - length
 kinematic viscosity, D thermal diffusivity,
c -specific heat
Emission of sound
probably the strongest
Damping

## Slide 13
Thermal expansion l(t)
substrate

## Slide 14
v0
v0<l+lT<w; 1D l, sound, 1D T
weak absorbers
ps pulses
l+lT<w<v0; 1D l (3D relaxation!), 1D T
Not a limit of 1D
Does not exist for stationary T
µs pulses, tight focusing
l+lT <v0<w; 1D l, 1D T
Valid for T-dependent parameters
ns pulses
w<lT< v0; 3D l, 3D T
I(r), D dependent, transient
local 3D focusing, µs-ms pulses
l +lT
laser
w
l
Notes: The meaning of the sound expression is clear – information about the expansion of subsurface layers does not reach the surface faster than the sound velocity.
The second 1D expression can be written in terms of fluence of intensity only due to Grüneisen proportionality between the thermal expansion and specific heat

## Slide 15
v0
v0<l+lT<w; 1D l, sound, 1D T
weak absorbers
ps pulses
l+lT<w<v0; 1D l (3D relaxation!), 1D T
Not a limit of 1D
Does not exist for stationary T
µs pulses, tight focusing
l+lT <v0<w; 1D l, 1D T
Valid for T-dependent parameters
ns pulses
w<lT< v0; 3D l, 3D T
I(r), D dependent, transient
local 3D focusing, µs-ms pulses
Difference
between approximations
can be significant
l +lT
laser
w
l
Notes: There can be different situations when this or that particular situation is relevant.
Besides, there can in principle be sound related effects, SAW, etc.

## Slide 16
Typical 1D surface displacement
Notes: What one has to remember, is that in 1D case velocity is intensity. Accelerations are about 106g. Two orders of magnitude more (?) may lead to destruction of material.

## Slide 17
Absorbing particle
(no thermal contact)
Transparent particle
(ideal thermal contact)
structures of expressions are always the same
Particle expansion r
Enters equations exactly as substrate expansion
Notes: Here several assumptions about equilibration of temperature and irrelevance of sound have been used, so this is all not for ps pulses. But for ns it is OK.
Particle substrate heat exchange is difficult, especially if we take into account that contact radius changes, etc.

## Slide 18
Cleaning threshold
3 Regimes exist
Elastic energy
Force or inertia
Kinetic energy

## Slide 19
Expansion 
compression 
(elastic energy) 
lift off after the pulse
Short pulse, big particle
particle doesn't move 
elastic energy
removal
Notes: Note that it does not depend on , because the pulse is instantaneous for such a heavy particle.
Note also the increasing dependence on r, as h0 increases in this way with r.
The potential is not completely symmetric, so that there are some additional numerical pre-factors here.

## Slide 20
Expansion
acceleration
deceleration/particle inertia
lift off due to decreasing I(t)
Long pulse, small particle
weak oscillations move 
force (inertial)
removal (also for damping)
Notes: Note very strong dependence on  (as it influences acceleration), and very bad dependence on r, which is due to competition between the volume forces r3 and adhesive forces r
In reality there are some coefficients dependent on pulse shape and also small excitation of oscillations introduces some numerical factor, that is difficult (and useless) to calculate.
The functional dependences are the most important

## Slide 21
Long pulse, small particle
short pulse fronts , velocity transfer 
kinetic energy
removal
Fast stopvelocity
particle inertia
lift off due to velocity
after the pulse
Velocity is important
Notes: We saw on the previous slide that the faster is deceleration, the better. The extreme case would be an instantaneous stopping of the substrate. In this case the particle acquires instantaneous velocity, and detachment criterion is written in terms of kinetic energy rather than force.
Note more advantageous r and  dependences.
Sound related effects set an ultimate limit to the rate with which the substrate can accelerate/decelerate.
It lies in the range of lT or l/vs~ 510-5/5105~100 ps for strong absorbers at least.
Leading front has less problems, as it is determined by l, while trailing front should “collect information” over the lT depth.

## Slide 22
3 CLEANING REGIMES
Excimer pulse
Second part, tf=100 ps
Damping increases cl, but keeps dependences
Notes: One can see here the 3 regimes discussed above.

## Slide 23
Pulse duration and material parameters
Excimer pulse
10 times shorter pulse
10 times lower adhesion
3 times softer materials
Notes: Pulse duration does not affect elastic regime
Young modulus does not affect force regime as pull-out force does not depend on elasticity, but on work of adhesion only.

## Slide 24
Comparison with experiments
N. Arnold et al., Proc. SPIE, 2001
Notes: It is important to realize, that the fluence cannot be made infinitely large as substrate damage starts. Homogeneous melting threshold is shown.
In reality local damage may start even earlier due to local field enhancement effects, that we will discuss later.

## Slide 25
RESONANT LASER CLEANING (RLC)
10 sinusoidal pulses, 100 MHz, no damping
Damping =0.20
Damping =0.50
Notes: In order to avoid damage, one can try to excite adhesion frequency resonantly. As intensity is velocity, it is enough to modulate the pulses.
Too many pulses is useless as damping and non-linearity of potential will prevent to use resonant effects in full.
Duration of each of 10 pulses is 10 ns, total duration is 100 ns. For the thermal problem at such a time scale it acts like single pulse with average intensity.

## Slide 26
Local 3D effects
Ablation, vaporization
3D thermal expansion
Local intensity distribution
Notes: Particle substrate heat exchange is difficult, especially if we take into account that contact radius changes, etc.

## Slide 27
Local intensity distribution
Large particle – geometrical optics. Small particle – dipole+plane wave
Exact -- numerical1, Mie2,3, Mie + substrate4,5
Advantages:
simple
holds for non-spherical shapes
Disadvantages:
fine effects are lost, but:
ns heat diffusion smoothens
intensity
1Rohrbach et al., J. Opt. Soc. Am. A, 98
2Münzer et al., Journal of Microscopy, 01
3Luk'yanchuk et al., Proc. SPIE, 01
4Luk'yanchuk et al., Proc. SPIE, 00
5Münzer et al., Proc. SPIE, 02
page
movie

## Slide 28
Mie calculations without substrate
A, B : 2r = 1.7 µm
C, D: 2r = 0.8 µm
E, F: 2r = 0.32 µm
The plot shows the intensity
I  E2
E, x
y
E
k
2.5 µm
H.-J. Münzer, A. Pack et al.: Journal of Microscopy 202 , 129 (2001)
(A,C,E)
(B,D,F)

## Slide 29
Large particle -- geometrical optics
Transparent particle
Absorbing substrate
We need surface Im
Caustic
spot wg r
intensity Im/I0 - independent on r, unlike in focus
Holds for deformed particles
r>>; n=1.5
I0
Im

## Slide 30
Small particle -- dipole
r=0.2; n=1.5; Ex-polariz.
spot wd r
additional 3D intensity Im/I0  r2
Holds also for non-spherical particles
Fine details are lost, no substrate
3D
spot wd r

## Slide 31
3D expansion: finite absorption 
Center of Gaussian beam, spot size w
Kernel for w/2=1

## Slide 32
Example: Si, “Nd-YAG2”, w/2=1, enhancement M=1
=1 J/cm2, FWHM=27 ns A=0.5, =2104 cm-1, w =1 µm
w
With surface absorptionw>>1
And small spot w2<< D

## Slide 33
1D+3D expansion
1D and 3D superimpose
3D is transient and faster
epicentral 3D (small contact area)
3 regimes still valid

## Slide 34
Dry Cleaning Threshold with Focusing and 3D expansion
dipole
geometrical
1D expansion
3-30 threshold decrease
weak effect for small r
no flattening of cl(r)
stronger 3D effects for large r, but:
T smaller due to low cl
Caustics, dipoles - holds for non spherical particles

## Slide 35
Comparison with the experiment
SiO2/Si, n=1.5
=248 nm
=27 ns
1D too small
3D OK
wrong slope:
local ablation
Schrems, Bäuerle et al. 2002

## Slide 36
Ablative cleaning thresholds
Based on the “evaporation” temperature reached for:
Substrate
Particle
Liquid
Requires solution of:
Optical problem
Thermal problem
Notes: Liquid if present

## Slide 37
Damage – common in DLC
Different materials, pulse lengths, wavelength
SiO2/Si, 1500 nm,
 = 500 mJ/cm²  cl
=1064 nm, 6 ns
PS/Si, 800 nm,  ~25 mJ/cm²
=800 nm, 30 ps
Mosbacher, Münzer et. al., Appl. Phys. A, 2001
Schrems, PhD thesis, Linz, 2002

## Slide 38
PS/Si, 800nm, f ~25 mJ/cm²
=800 nm
100 fs
8 ns
Al2O3/Si, 400 nm
=800 nm
800 nm
fs holes better localized
Irregularly
shaped particles:
150 fs
Leiderer, Boneberg, et al, Proc. SPIE, 2000
Münzer, Mosbacher, et. al, Proc. SPIE, 2002

## Slide 39
Focusing of sagittal rays  central caustic line (here in Mie calculations*)
*Program by Wang, Luk’yanchuk, DSI Singapore
Spherical particle

## Slide 40
Intensity under a SiO2 particle r = z =3.1 µm n=1.4, =248 nm. Mie parameter kr=78.54.
Central caustic line*
Ic~kr, wc~/5, P/P~(kr)-1
Caustic cone*
Ico~(kr)1/3, wco~2/3r1/3, P/P~(kr)-1/3
stable
Geometrical region
Ig~C(n), wg~r, P/P~1
What determines Tmax depends on pulse duration 
*based on: Kravtsov, Orlov
Caustics, catastrophes and wave fields, 1998
Shadow

## Slide 41
Intensity under the particle: Comparison with Mie results
Luk’yanchuk, Arnold, Huang, Wang, Hong., Appl. Phys. A, 2003
Central intensity
Ic /I0  r/
spot wc~ /5
Mie resonances
(smeared out by imperfections)
Notes: Mie resonances smeared out by size distribution, shape changes, defects, absorption

## Slide 42
Heating of particle
“Transparent” particles
Very large particles pr>>1
absorption
heat exchange with the substrate

## Slide 43
Local 3D effects*
Thermal expansion
cleaning threshold
Ablative
cleaning threshold
Intensity
Dynamics of particle
3D thermal expansion
Local ablation ~1.5Tb,
momentum transfer
Temperature
*Luk’yanchuk, Arnold, et al, Appl. Phys. A, 2003
Notes: Particle substrate heat exchange is difficult, especially if we take into account that contact radius changes, etc.

## Slide 44
Feasibility of ablative cleaning of particles
Actual pressures higher (lateral expansion, losses)
Such pressures are attainable within narrow interval of Tmax~1.5 Tb
Force criterion: pS>Fadhesion
Energy criterion pV>Eadhesion
Conditions for the pressure p
Notes: Liquid if present

## Slide 45
Focusing: intensity and temperature
ns pulses, r>3:
Imax due to caustic
Tmax due to geom.
(larger power)

## Slide 46
Comparison with the experiment SiO2/Si, ablative mechanism
- KrF, =248 nm, Vacuum*
=27 ns, A=0.39, l=6 nm, lT=0.8 µm, np=1.5
3D calculations
Thermal expansion - wrong
Ablation-correct slope
Discrepancies:
Substrate influence
Parameters (T-dep., particles stoichiometry)
*Schrems, Mühlberger, et. al, 2002
Rescaled to Mie

## Slide 47
Nd-YAG2, =532 nm, Vacuum*
=8 ns, A=0.63, l=0.1 µm, lT=0.45 µm
, lT , l, r/ , A change 
3D part different
Ablation - correct slope
*Bertsch, Mosbacher, et. al, 2002

## Slide 48
Nd-YAG, =1064 nm, Vacuum*
=8 ns, A=0.7, l=17 µm, lT=0.45 µm
Strong (T)
Large uncertainties, but
Ablation-correct slope
*Schrems, Bäuerle et al. 2003

## Slide 49
Steam laser cleaning (SLC)

## Slide 50
Cleaning in vapor atmosphere
Steam laser cleaning:
Explosive evaporation of thin liquid layer
Removes small particles, but:
poor reproducibility
Spin-on, film inhomogeneities
film unstable - evaporates, difficult to control,
synchronization with the laser pulse
Contaminates all surface
Use capillary condensation
occurs below 100% relative humidity (RH)
stable liquid meniscus
liquid is only where it is needed
Kelvin
Radius RK

## Slide 51
Kelvin Radius RK
Decrease of evaporation energy per molecule due to curvature K
Saturated pressure over concave surface=ambient pressure ps(K)=pRH ps(0)
With relative humidity RH<1 curvature K is negative (concave meniscus)requires more than 1 surface
Similar to critical nucleus – extremum of free energy
For “void” capillary geometry meniscus is stable for condensation/evaporation

## Slide 52
Capillary condensation
S1
Vl
RK
r
Liquid-particle surface
Liquid volume (wetting)
Capillary adhesion force
Independent on RH
Meniscus is stable. Kelvin radius:
 - surface tension, µ - molar weight
Notes: Note linear dependence on r

## Slide 53
Experimental Setup
pump
cooling
trap
distilled water
entrance window
target
reaction
chamber
valve
valve
KrF laser
pulse
93%  RH  97%
25°C  T  28,5°C
31mbar  p  35mbar
hygrometer
thermometer
barometer

## Slide 54
KrF, =248 nm, RH vs Vacuum*
=27 ns, np=1.5, RH0.95
*Schrems, Bäuerle et al, 2003
With RH:
Larger particles cl~const
Smaller particles cl
Tclean gradually decreases
Why?
holes with large particles remain

## Slide 55
Water meniscus drawn in scale
n=1.4, RH=0.95
Kelvin radius RK=10 nm
Vwater>Vablated material for smaller r
turnover at:
Size r= 2.5 µm
Size r= 0.15 µm
Note that:
Surface tension disappears near Tc l
water in the interstice
decreases adhesion ~10 times
Notes: One can think of a tricky mechanism: Water a) increases adhesion by adds capillary force b) decreases adhesion as such by decreasing work of adhesion by polar molecules. When everything is cold, adhesion is increased, via capillary. But as we heat near critical temperature, capillary contribution disappears due to vanishing surface tension and we are left with pure decrease of adhesion.

## Slide 56
Conclusions for cleaning with RH0.95
Large particles (2r=5000, 3280 nm)
Ablation of substrate is dominant 
cl const(RH)
Small particles (300 nm – 800 nm)
Removed more efficiently in RH - large contribution of explosively vaporized water

## Slide 57
2r=5 µm SiO2
Particles on Si,  = 383 mJ/cm²
2r =3.28 µm SiO2
Particles on Si,  = 350 mJ/cm²
KrF, =248 nm, 27 ns
RH 0.95
Large particles
still produce holes*
*G. Schrems, Ph.D. thesis, Linz (2003)

## Slide 58
Let us draw it in scale
n=1.4
Note that:
Surface tension disappears near Tc l
water molecules in the interstice may
decrease adhesion by a factor of ~100
Heating up to below Tc l may help
RH=0.99 Kelvin radius RK=50 nm
r= 2.5 µm
r= 150 nm
r= 150 nm
r= 50 nm
RH=0.95, Kelvin radius RK=10 nm
There is a difference between RH=0.95 and 0.99
Notes: One can think of a tricky mechanism: Water a) increases adhesion by adds capillary force b) decreases adhesion as such by decreasing work of adhesion by polar molecules. When everything is cold, adhesion is increased, via capillary. But as we heat near critical temperature, capillary contribution disappears due to vanishing surface tension and we are left with pure decrease of adhesion.

## Slide 59
saturated salt, glycerol
or sulfuric acid solutions
entrance
window
target
thermostatic
reaction chamber
valve
laser
pulse
hygrometer
thermometer
barometer
How to achieve stable high RH~1 : desired experimental setup
saturated salt, glycerol or sulfuric acid solutions*
*From: F. Restagno, PhD thesis, Lyon, 2000
R. C. Weast. CRC Handbook of Chemstry and Physics
Also*: At 20 °C:
Pb(NO3)2 RH=98
CuSO4.5H2O RH=98
H2SO4: 1.051, RH 97.51

## Slide 60
Cleaning with laser-excited SAW (surface acoustic waves)

## Slide 61
Cleaning with laser-excited
1D SAW (surface acoustic waves)
SAW cleaning outside the beam
was demonstrated
Advances in theory
Field enhancement 
Local ablation 
Damage
Difficult to modulate
Resonant laser cleaning (RLC) idea
No light – no damage
Interference1D
GHZ possible
Recovered

## Slide 62
SAW cleaning with focused pulses*
*A. A. Kolomenskii, H. A. Schuessler, V. G. Mikhalevich, and A. A. Maznev, J. Appl. Phys., 84(5) 2404 (1998)
A. A. Kolomenskii, A. A. Maznev, Phys. Rev. B., 48(19) 14502 (1993)
1-2 µm Al2O3 on (111) Si, in air
Nd:YAG-1.06 µm, 10 ns,10 pulses
1-10 µm Al2O3 on (100) Si, in air
N2-337 nm, 10 ns, 50 pulses
SAW wavelength is determined by the spot size ~ 15 µm
SAW is 2D and decays fast
SAW has 1-2 oscillations only
Cleaning of the particles outside of irradiated area, enhanced along the lines where SAW is stronger

## Slide 63
180 ps, THG Nd:YAG (335 nm), Si
SAWs excited with
ps-pulse interference*
100 MHz frequency =0.8° easily varied up to 1-10 GHz**
Many oscillations - resonance
1D propagation out of the beam area
No light – no damage
Non-linear effects, larger acceleration
Breakdown in air, universality
*A. Frass, A. Lomonosov, P. Hess, V. Gusev, J. Appl. Phys., 87(7) 3505 (2000)
**R. M. Slayton, K. A. Nelson, A. A. Maznev, J. Appl. Phys., 90(9) 4392 (2001)

## Slide 64
SAW are 1D. No fast decay, propagate out of the beam area.
No light is present in the majority of area covered by SAWNo local field enhancement-damage.
SAW have many oscillations, suitable for testing of RLC
Frequency is determined by the periodicity of interference. vSAW~vsound/light~1-10 GHz - suitable for resonant laser cleaning (RLC).
Frequency easily varied via angle of interfering beams. Indispensable for testing and application of RLC.
Smaller overall thermal load on the substrate.
Non-linearity makes fronts steeper, increase accelerations.
Can be excited via breakdown in the air. Material independent, suitable for structured substrates, (industry).
Advantages of 1D SAW excited by laser light interference for cleaning

## Slide 65
Influence of storage time

## Slide 66
Influence of storage time*
Cleaning threshold strongly depends on storage time,
especially for larger particles
*G. Schrems, M. P. Delamare, et al. 2002

## Slide 67
Visible deformation, larger contact area, therefore stronger adhesion
17 h
1350 h
SiO2/Si, 1500 nm
Reasons: possible formation of covalent bonds:
Hydroxyl groups – hydrogen bonds – water loss – formation of covalent bonds –Si–O–Si–
stronger adhesion – stronger deformation – larger contact area – even stronger adhesion
Possible plastic deformation
Additional oxidation

## Slide 68
Storage time: threshold dependence
1500 nm particles: threshold doubles
Small times are necessary for reproducible experiments