## Slide 1
THEORETICAL SUGGESTIONS
FOR THE IMPROVEMENT OF DRY LASER CLEANING
N. Arnold
Angewandte Physik, Johannes - Kepler - Universität
A-4040, Linz, Austria

## Slide 2
Summary:
Optimal absorption and pulse duration for damage-free DLC
Cleaning in high RH atmosphere
Cleaning by 1D laser-induced SAW
Motivation and goals
DLC is simple but not very efficient
Theoretical understanding improved over the last years
Local damage hinders DLC
Discuss qualitative ideas that can help DLC

## Slide 3
Optimal absorption length
and pulse duration for DLC
We want to clean small particles by DLC
Field enhancement  Local ablation  Damage
One should not heat more than Tm
One should make expansion larger  l
But not so large, that sound slows expansion
To decrease enhancement: r/ if r  and 
Convert these considerations into formulas

## Slide 4
For non-absorbing particles
Smaller substrate absorption (bigger l) is better
for damage-free cleaning
Smaller absorption, shorter pulses
or why Excimers are bad for DLC
Why?
l larger  with the same surface temperature Ts < Tmelting ,
expansion l Tdz larger  larger cleaning-damage window
T(z)
Ts<Tm

## Slide 5
Small particles are interesting
They are removed in the force regime ml/ 2>F0 2r
If r<< , they weakly disturb the local field (small dipole moment)
Even if they do, l3D < l1D for equal parameters and Ts
At best, maximum expansion till surface melting lmax 1Tm(l+lT)
Force threshold written for l:
Almost universal constant
Sizes that can be removed
 - work of adhesion per area

## Slide 6
in µm, ns:
 =100 ps
l=1 µm
Q-switch
l=100 µm
Excimer
l=10 nm
Try Er or other IR with  <1 ns
r/ is also better for IR
c-Si:
l(193,248,308)5-10 nm
l(1.06)  200 µm50 nm
l(2.94)  500 cm30 µm
(depending on doping and T)
l(10.6)  1000 µm100 nm
Experiments with Nd:YAG – still damage.
Talk of Prof. Bäuerle and poster of G. Schrems

## Slide 7
Cleaning in vapor atmosphere
Steam laser cleaning:
Explosive evaporation of thin layer of liquid
Removes small particles, but:
poor reproducibility
Spin-on, film inhomogeneities
film unstable - evaporates, difficult to control,
synchronization with the laser pulse
Contaminates all surface
Use capillary condensation
occurs below 100% relative humidity (RH)
stable liquid meniscus
liquid is only where it is needed
Kelvin
Radius RK

## Slide 8
Capillary condensation
S1
Vl
RK
r
Liquid-particle surface
Liquid volume (wetting)
Capillary adhesion force
Independent on RH
Meniscus is stable. Kelvin radius:
 - surface tension, µ - molar weight
Notes: Note linear dependence on r

## Slide 9
Let us draw it in scale
n=1.4
Note that:
Surface tension disappears near Tc l
water molecules in the interstice may
decrease adhesion by a factor of ~100
Heating up to below Tc l may help
RH=0.99 Kelvin radius RK=50 nm
r= 2.5 µm
r= 150 nm
r= 150 nm
r= 50 nm
RH=0.95, Kelvin radius RK=10 nm
There is a difference between RH=0.95 and 0.99
Notes: One can think of a tricky mechanism: Water a) increases adhesion by adds capillary force b) decreases adhesion as such by decreasing work of adhesion by polar molecules. When everything is cold, adhesion is increased, via capillary. But as we heat near critical temperature, capillary contribution disappears due to vanishing surface tension and we are left with pure decrease of adhesion.

## Slide 10
Experiments with different setup, RH~95%:
Talk of Prof. Bäuerle and poster of G. Schrems
saturated salt, glycerol
or sulfuric acid solutions
entrance
window
target
thermostatic
reaction chamber
valve
laser
pulse
hygrometer
thermometer
barometer
How to achieve stable high RH~1 : desired experimental setup
saturated salt, glycerol or sulfuric acid solutions*
*From: F. Restagno, PhD thesis, Lyon, 2000
R. C. Weast. CRC Handbook of Chemstry and Physics
Also*: At 20 °C:
Pb(NO3)2 RH=98
CuSO4.5H2O RH=98
H2SO4: 1.051, RH 97.51

## Slide 11
Cleaning with laser-excited
1D SAW (surface acoustic waves)
SAW cleaning outside the beam
was demonstrated
Advances in theory
Field enhancement 
Local ablation 
Damage
Difficult to modulate
Resonant laser cleaning (RLC) idea
No light – no damage
Interference1D
GHZ possible
Recovered

## Slide 12
SAW cleaning with focused pulses*
*A. A. Kolomenskii, H. A. Schuessler, V. G. Mikhalevich, and A. A. Maznev, J. Appl. Phys., 84(5) 2404 (1998)
A. A. Kolomenskii, A. A. Maznev, Phys. Rev. B., 48(19) 14502 (1993)
1-2 µm Al2O3 on (111) Si, in air
Nd:YAG-1.06 µm, 10 ns,10 pulses
1-10 µm Al2O3 on (100) Si, in air
N2-337 nm, 10 ns, 50 pulses
SAW wavelength is determined by the spot size ~ 15 µm
SAW is 2D and decays fast
SAW has 1-2 oscillations only
Cleaning of the particles outside of irradiated area, enhanced along the lines where SAW is stronger

## Slide 13
180 ps, THG Nd:YAG (335 nm), Si
SAWs excited with
ps-pulse interference*
100 MHz frequency =0.8° easily varied up to 1-10 GHz**
Many oscillations - resonance
1D propagation out of the beam area
No light – no damage
Non-linear effects, larger acceleration
Breakdown in air, universality
*A. Frass, A. Lomonosov, P. Hess, V. Gusev, J. Appl. Phys., 87(7) 3505 (2000)
**R. M. Slayton, K. A. Nelson, A. A. Maznev, J. Appl. Phys., 90(9) 4392 (2001)

## Slide 14
SAW are 1D. No fast decay, propagate out of the beam area.
No light is present in the majority of area covered by SAWNo local field enhancement-damage.
SAW have many oscillations, suitable for testing of RLC
Frequency is determined by the periodicity of interference. vSAW~vsound/light~1-10 GHz - suitable for resonant laser cleaning (RLC).
Frequency easily varied via angle of interfering beams. Indispensable for testing and application of RLC.
Smaller overall thermal load on the substrate.
Non-linearity makes fronts steeper, increase accelerations.
Can be excited via breakdown in the air. Material independent, suitable for structured substrates, (industry).
Advantages of 1D SAW excited by laser light interference for cleaning

## Slide 15
Singapore
Prof. B. Luk’yanchuk, Prof. Y.F. Lu, Dr. M. Hong, Dr. Z. B. Wang
Konstanz
Prof. P. Leiderer, Dr. M. Mosbacher, Dr. H. Münzer, DI. M. Olapinski
Sydney
Prof. D. Kane, Dr. S. Pleasants
Linz
Prof. D. Bäuerle, Dr. M.P. Delamare, DI. G. Schrems, Dr. K. Piglmayer
Funding:
Austrian Science Fund (FWF), P14700-TPH
EU TMR Laser Cleaning, #ERBFMRXCT98 0188
Acknowledgments (discussions, ideas, pictures)
College Station, Heidelberg
Prof. A. Kolomenskii, Prof. P. Hess, A. Maznev