## Slide 1
TRANSMISSION THROUGH COLLOIDAL MONOLAYERS WITH AN OVERLAYER – A THEORETICAL CONSIDERATION
N. Arnold
Angewandte Physik, Johannes - Kepler - Universität
A-4040, Linz, Austria

## Slide 2: Summary
History and motivation
Transmission of bare colloidal monolayers
  Rayleigh-Wood anomalies in diffraction
a-Si covered monolayers
  Photonic crystals
  Mode profiles and coupling
Metal covered monolayers
  Minimal model of plasmon-mediated transmission

## Slide 3: History and motivation
Patterning in Laser Cleaning and with ML arrays (Konstanz, Singapore)
Arrays of microspheres on support used for processing (Linz)  need to understand the bare ML transmission properties
a-Si covered spheres for light manipulation  need to understand the transmission properties with the Si overlayer
Metal coated spheres for LIFT and apertured spheres arrays  need to understand plasmonic effects

## Slide 4: Transmission measurements
Spectrometer
Far field, direct transmission (normal or oblique)
Not a laser light
Non-polarized
Monolayer domains in irradiated area

## Slide 5: Bare SiO2 monolayer
Dip: wavelength scales with d: d/~1.12
No order - no dip
Decrease at small:
Diffraction grating, interference from a “primitive cell”:

## Slide 6: Rayleigh-Wood anomaly
Known in gratings of all types. Diffracted waves at the grazing angle  couple  consume energy
Energy conservation  dip in zero order (normal transmission)
Large-angles  requires full 3D vector Maxwell equations.
b
k’=k+b
k
k
k


## Slide 7: Dip condition
Bragg condition:
Normal incidence, 1st order diffraction, possibility to couple
a1
a2
b2
b1
M
K

b - reciprocal lattice (2D hexagonal)
Effective nmon from the filling factor f ≈ 0.6
and mixing law for  :
Notes: f=Pi/3 sqrt(3)

## Slide 8: FDTD calculations
λ/d=0.8
λ/d=1.0
Notes: Full vector FDTD calculations of the light coupling into the monolayer of dielectric spheres with n=1.42, d=1.42 µm. Normally incident excitation field is polarized in z-direction and has a Gaussian profile with the (1/e field) width w0=5 µm centered at x=-3 µm

## Slide 9: FDTD calculations
λ/d=1.2
λ/d=1.1
dip
Notes: Full vector FDTD calculations of the light coupling into the monolayer of dielectric spheres with n=1.42, d=1.42 µm. Normally incident excitation field is polarized in z-direction and has a Gaussian profile with the (1/e field) width w0=5 µm centered at x=-3 µm

## Slide 10: a-Si covered monolayers
Transmission spectrum:
Main dip deepens and red shifts with increasing thickness
Multiple dips appear
L. Landström, D. Brodoceanu, N. Arnold, K. Piglmayer and D. Bäuerle, Appl. Phys. A. 81, 911 (2005).

## Slide 11: Relation to photonic crystals
ML with the overlayer = photonic crystal slab (PCS) with high contrast (like inverted opal) (3<nSi<5)
Dip = diffracted wave couples to the mode
Multiple modes  multiple dips
Normal incidence: θ=0  dips corresponds to the ω d/ λ of the lowest modes at the center (Γ-point) of the Brillouin zone in the (multi-valued) frequency surface ω(k)
Confined modes – periodic in-plane, evanescent in z-direction – no good software  use supercells, filter out folded modes
a1
a2
b2
b1
M
K


## Slide 12: Computational scheme
# 20 true
# 22 folded
Smoothened ε profile
Plane wave expansion
Deposit – shifted spheres
h/d=0.2, support included
Supercell 5d in z-direction
Modes at Γ-point
True vs. folded modes:
Structure
Si-confinement  h-dependence
Supercell dependence, number

## Slide 13: Dependence on the overlayer thickness
L. Landström, N. Arnold, D. Brodoceanu, K. Piglmayer and D. Bäuerle, Appl. Phys. A. 83, 271 (2006).
Squares – experimental dip positions
Estimation with neff
Notes: Frequencies of the lowest modes at Γ -point as functions of a-Si deposit thickness h. Only
confined (not folded) modes are shown. Dotted curve – estimation from (2) (at normal incidence θ = 0)
and (3). Experimental points are deduced from the dips (solid squares) and maxima (open circles) in the
transmission curves for the microspheres with d = 1.42 μm. nSiO2 = 1.35 and 1.42 were taken for the
spheres and support, respectively, nSi = 3.3 for the a-Si layer of thickness h was used
Only true modes are shown

## Slide 14: Mode profiles
Lowest “donut” mode
From lowest ML mode at h=0, has azimuthal E structure
Weak coupling (FDTD)
“Main dip” mode
6-fold symmetry
Good coupling into 6 waves
Modes are mainly in Si deposit (larger n)
h/d=0.175
Notes: Distribution of intensity EE∗ in two of the modes at the Γ -point. Deposit thickness
h = 0.175d. (a) Donut mode; (b) The mode tentatively responsible for the most pronounced dip in
transmission. Other parameters are as in Fig. 4

## Slide 15: FDTD coupling
h/d=0.175, nSiO2=1.35, spheres, nglass=1.42, nSi=3.3
Ez ↕ (incident) component shown
Dip is broad in λ, several coupling modes
λ/d=1.54
Measured dip
λ/d=1.87
donut
λ/d=1.24
Measured maximum
Notes: Full vector FDTD calculations of the light coupling into the monolayer of dielectric spheres
of thickness d on the quartz support (nquartz = 1.35 and 1.42 was taken for the spheres and
support, respectively). nSi = 3.3 for the deposited a-Si layer of thickness h was used. Normally
incident Gaussian beam has half-width (1/e field) w0 = 2.5d , is centered at x = −2d, z = −2d,
and is polarized in z-direction. Ez component is shown everywhere. a) h = 0, λ/d = 0.75. b)
h/d = 0.175, λ /d = 1.87 , donut mode, see FIG. 4a. c) h/d = 0.175, λ /d = 1.54, main measured
dip, see FIGS. 1, 3 and 4b. d) h/d = 0.175, λ /d = 1.22, measured transmission peak, see FIGS. 1
and 3.

## Slide 16: Effective refractive index
Main dip position: neff↑  ω~d/λdip↓
n(λ) neglected here
Estimation with neff
Notes: Frequencies of the lowest modes at Γ -point as functions of a-Si deposit thickness h. Only
confined (not folded) modes are shown. Dotted curve – estimation from (2) (at normal incidence θ = 0)
and (3). Experimental points are deduced from the dips (solid squares) and maxima (open circles) in the
transmission curves for the microspheres with d = 1.42 μm. nSiO2 = 1.35 and 1.42 were taken for the
spheres and support, respectively, nSi = 3.3 for the a-Si layer of thickness h was used
Only true modes are shown

## Slide 17: Oblique incidence
Main dip splits in two
Different directions describe frequency surface dispersion ω(k) near the Γ-point
Non-idealities:
ML domains ~100 μm, non-polarized light  orientation averaging
Various sizes, defects, 3<nSi<5
Coupling coefficients
Simplified neff description
 point
Notes: Changes in zero-order
transmission with the angle of incidence
θ. a-Si deposit thickness h = 0.11d with d = 1.42 μm. The points
in the inset (squares) are deduced
from the transmission dip positions
in the main plot. Transmission curves
are shifted in y-scale for convenience

## Slide 18: Orientation-dependent coupling
Main dip mode. Use neff near Γ-point (normal incidence)
Different directions (φkb angle) describe frequency surface dispersion ω(k)
Observed transmission is averaged over different orientations φ and polarizations
φ
Notes: FDTD calculations of the light coupling into composite monolayer. Material parameters
as in Fig. 2. Field component corresponding to the polarization of incident Gaussian beam ( or ↔) is
shown at y = 0.5d (top of the spheres). Beam with half-width (1/e field) w0 = 2.5d centered at x =−2d,
z=−2d and at x =−2d, z = 0 for (c). (a) Normal incidence, h/d = 0.175 and λ/d = 1.54. This corresponds
to the main measured dip seen in Fig. 1. Its h dependence is shown in Fig. 2 and the responsible
mode in Fig. 3b. (b) Same as (a) but for λ/d = 1.22, corresponding to transmission maximum seen in
Figs. 1 and 2. (c) Oblique incidence (θ = π/6 in x–y plane). h/d = 0.11 and λ/d = 1.6. Diffraction on
b vector with ϕ = π is responsible for the lowest dashed curve in the inset in Fig. 5. (d) Same as (c) but
λ/d = 1.23. Strong diffraction on 2 b vectors with ϕ=±π/2 is responsible for the upper curve in Fig. 5
(inset)

## Slide 19: FDTD coupling and polarization
θ=π/6, h/d=0.11
Better coupling to ks  E
Dipole effect
Note change in mode period
λ/d=1.23, Ex ↔ shown
φ=π/2, strong
φ=π/2, weaker
λ/d=1.6, Ez ↕ shown
φ=π, strong
φ=5π/6, weaker
Notes: Full vector FDTD calculations of the light coupling for oblique incidence θ = π /6 in
x − y plane. Beam center is at x = 2d, z = 0 and h/d = 0.11. Other parameters as in FIG. 2. a)
λ/d = 1.23, p-polarization, Ex component. Strong diffraction on 2 mathbfb vectors with φ = ±π/2
corresponds to the upper curve in the inset in FIG. 5. b) λ /d = 1.23, s-polarization. Ex-component
of the field results from the scattering on the spheres light couples into the same modes as in
a), albeit somewhat weaker. c) λ /d = 1.6, s-polarization, Ez component. Strong diffraction on
mathbfb vector with φ = π. d) λ /d = 1.6, p-polarization, Ez component. Diffraction on 2 mathbfb
vectors with φ = ±5 π /6 (s-polarization couples even stronger). Cases c) and d) correspond to two
lower curves in the inset in FIG. 5.

## Slide 20: Metal-covered monolayers
Transmission spectrum:
Metal independent
Bare monolayer minima become maxima
Slightly red shifted
Positions thickness independent
high T values (compare dash and dash-dot)
L. Landström, D. Brodoceanu, K. Piglmayer, G. Langer and D. Bäuerle, Appl. Phys. A. 81, 15 (2005).
max scales with d 1st maximum: d/~1.18
Notes: Transmission spectra measured at normal incidence for monolayers of a-SiO2 microspheres
(d ≈ 1.4 μm) coated with different metals. The dash-dotted curve shows the spectrum for
a 75 nm thick Ag film on a plane a-SiO2 substrate

## Slide 21: Minimal model
1, monolayer nmon
3, air
2, metal
t23
t12
r23
r21
Question: Why metal transmits?
Metals: Re <0, FDTD requires 200 points/
Time consuming  minimal model – Metallic Fabry-Perot
Ec
Et
1
2
3
h
Ei
Er
Standard FP, but:
Evanescent waves
In and out coupling by diffraction: t01 means from 0 to 1st order, etc.
L. Martín-Moreno, F.J. García-Vidal, H.J. Lezec, P.M. Pellerin, T. Thio, J.B. Pendry, T.W. Ebbesen, Phys. Rev. Lett. 86, 1114 (2001).

## Slide 22: Resonant FP denominator
Transmission large when denominator small
Can happen despite exponential term
For evanescent waves Fresnel coefficient r>>1 is possible
2=metal=-143.75+12i (~Ag)
3=air=1 and 1=mon=1.81
metal-air
metal-monolayer
p-polarization
evanescent

## Slide 23: Qualitative transmission (denominator)-1
p-polarization
s-polarization
Ag, h=30 nm
Main maximum-metal-monolayer
For quantitative description:
Many modes together
Coupling coefficients t difficult
Better FDTD

## Slide 24: Plasmons and minima to maxima inversion
Resonant r>>1 condition <> surface plasmon on the interface
1st order diffraction, normal incidence, metal-monolayer interface
Almost = bare ML dip condition
Upper part of the ML contains no air 
filling f=0.8>0.6  nmon↑  λdip↑ 
minima become maxima that are red shifted (λ/d=1.18 vs. 1.12) (holds for SiO2 and PS spheres)

## Slide 25: Multiple maxima positions
Oblique incidence, higher order diffraction:
Maxima are broad, overlap
Orientation averaging
All ε depend on λ
Coupling coeffs. t differ
Difficult to say if metal-air interface plays a role
metal-monolayer and metal-air
metal-monolayer
Normal incidence, Ag

## Slide 26: Interesting experimental question
Does one need the holes in the metal to see extraordinary transmission?
Or film modulation alone is enough?
The (qualitative) theoretical answer:– it shall work without holes
Difficult to verify (smaller efficiency, cracks)

## Slide 27: Acknowledgements
Prof. D. Bäuerle
Dr. L. Landström
Dr. K. Piglmayer
CD Laboratory for Surface Optics
Univ. Doz. Dr. K. Hingerl
MSc. J. Zarbakhsh
Funding:
Austrian Science Fund (FWF), P16133-N08